## Slide 1
Investigation of Turn-on and Turn-off Characteristics of Enhancement-Mode
GaN Power Transistors
Abstract
Furkan Karakaya
(furkan.karakaya@metu.edu.tr)
Steady State Results of the Model
Ozan Keysan
(keysan@metu.edu.tr)
PowerLab Research Group, METU, ANKARA
Mesut Ugur
(ugurm@metu.edu.tr)
In this paper, turn-on and turn-off switching behaviour of 650V enhancement-mode GaN power FETs are investigated. An analytical model is developed to analyse the current-voltage characteristics of the device during switching transients both with and without the effects of parasitic components. In addition, the effect of the temperature and circuit parameters on the switching characteristics are investigated.
GaN Modeling
Fig. 1: The hybrid model of e-mode GaN power FET
Fig. 2: Parasitic capacitances vs Drain-Source Voltage plot (a) & Input Capacitance vs Gate-Source Voltage plot (b)
(a)
(b)
Even though manufacturer provides the Ciss as constant with respect to drain-source voltage, it changes significantly with varying gate-source voltage. Implementing this feature in the model is important to obtain accurate dynamic/switching characteristics.
(a)
(b)
Fig. 3: Static Results of GS66508B for Forward Conduction (a) & Reverse Conduction (b)
The reverse conduction behaviour is highly dependent on the applied gate voltage. A negative gate bias increases the reverse conduction loss. Therefore, the negative gate bias level and dead-time duration optimization is very critical for especially high frequency switching applications.
Fig. 3: Thermal characteristics of GS66508B obtained by the model for forward conduction at 6V gate-source voltage
Blue branch indicates the device channel
The parasitic capacitances are highly dependent on the electrical field between drain-source terminals.
Kelvin Source (SS) pin is used to eliminate Common Source Inductance (CSI) which might cause the device failure.
Junction temperature is a key factor which affects the trans-conductance of the device
The trans-conductance is nearly halved for every 75ºC increase in junction temperature
Switching Test Circuit Configurations
Fig. 4: Double Pulse Test (DPT) Circuit Configuration
The circuit is implemented in MATLAB / Simulink® platform to investigate switching transients.
Input voltage (Vd) | 400 V | Internal gate resistance (Rg) | 1.5 Ω | Gate parasitic inductance (Lg) | 3.0 nH
Output Current (ILOAD) | 20 A | Drain/source inductances (Ls) | 0.9 nH | Power loop inductance (Lp) | 7.0 nH
Load inductance (LLOAD) | 35 mH | Turn-on gate resistance (RG-ON) | 10 Ω | Junction Temperature (TJ) | 125 0C
Applied gate voltage (Vgs) | -3V/+6V | Turn-off gate resistance (RG-OFF) | 1 Ω | Dead-time (tdead) | 20 ns
Table 1: The parameters used for the test circuit in MATLAB / Simulink ®